## Slide 1
Derryl Poynor
Rick Steffe
David Cunningham
Ti-6Al-7Nb
Hip Prosthesis
(Femoral Hip Stem)
Notes: Introduction: Time, use, and accidents can wear on our bodies until they no longer function. Then what do you do? Using their vast knowledge of metals, properties, and manufacturing, engineers and metallurgists have recreated some of these structures that are compatible to work within our body. A very common problem in older people is worn hips. We use our hips all of the time even when we are lying down. One of the structures created is a hip replacement, or more specifically the femoral component of a hip prosthesis. It is made of the alloy Ti-6Al-7Nb.
Explain the picture of the hip prosthesis and compare the two pictures

## Slide 2
Composition
Impurities
  Ta: < 0.5%
  Fe: < 0.25%
  N2: < 0.05%
  O2: < 0.2%
  C: < 0.08%
  H2: < 0.009%
Chart: 
| Titanium | Aluminum | Niobium | Impurities
Ti-6Al-7Nb | 85.911 | 6 | 7 | 1.089
Notes: Explain how Ti-6Al-7Nb explains its percentage of alloys and why each elements purpose is
Titanium is biocompatible, corrosion resistance, low density, and a similar elastic modulus to bone
Aluminum is an alpha stabilizer
Niobium is a beta stabilizer and more compatible than vanadium. (Explain that Ti-6Al-4V is also used)
State the impurities
  Impurities
      Causes alloy to assimilate undesirable properties
      Fit into the gaps between larger molecules
      Comes from air and molds
    Ta: < 0.5%
    Fe: < 0.25%
    N2: < 0.05%
    O2: < 0.2%
      Lowers fracture toughness
      Has a very high affinity for titanium
    C: < 0.08%
      Reduces ductility
      Increases overall strength
    H2: < 0.009%
Explain how the impurities do not physically affect the molecular structure (refer to drawing), but instead give the alloy the properties

## Slide 4
Superior Atmospheric Corrosion
Allotropic
Highly Reactive Metal Surface
BIOCOMPATIBLE!
  Cells accept alloy
  High protein absorption
  Inert coating
Chemical Properties
Notes: Atmospheric Corrosion- prevents from being deteriorated from elements, such as oxygen.
Allotropic- Explain what that is (Alpha-beta alloy that transitions to beta at 1850oF)
Explain the molecular structure of both (refer to picture)
Highly reactive Metal Surface – Naturally bonds with oxygen to form an inert coating (helps with biocompatibility)
Biocompatible- (Explain during next slide)

## Slide 5
http://ars.els-cdn.com/content/image/1-s2.0-S0169409X10000402-gr2.jpg
Notes: Biocompatibility means high protein absorption, inert surface, and cells accept the alloy.
The protein must absorb proteins in order to fool the immune system that the hip prosthesis is “SELF” (implant needs a porous surface)
Inert surfaces means that the implant won’t release toxins into the body or react with other elements
Cells accept the alloy means that the immune system wont attack the implant, causing inflammation and rejection.
Explain the picture

## Slide 6
Stress/Strain
Tensile strength is 145ksi
Hardness values
  Rockwell A – 66.5
  Rockwell C – 32
High compressive strength is 156-158 ksi
Elongation is 9.4 – 13.2%
Fracture toughness is 61.9 – 68.3 ksi. in1/2
Fatigue Strength is 72500 psi
Yield Strength is 114 – 130 ksi
Notes:     Tensile strength is 145ksi
    Hardness values
      Rockwell A – 66.5
      Rockwell C – 32
      Rockwell D – 49.0
    High compressive strength (156-158 ksi)
      Must withstand weight and movement of recipient
    Elongation (9.4 – 13.2%)
    Only matters if you jump off of a building
    Fracture toughness
      61.9 – 68.3 ksi. in1/2
    Resists cracks from getting worse
    Isn’t as high as it ideally should be
    Fatigue Strength
      72500 psi (10 Million Cycles, Rotating bend motion)
      Lasts a long time (10 year guarantee)
      Can handle pressure from being applied and released continually
    Yield Strength (114 – 130 ksi)

## Slide 7
Physical Properties
Ductile
Low density
Low friction
Notes:   Mechanical & Physical Properties
    ½ Density of steel
      Density is 4.52g/cm3
      Lightweight like a bone
      Still weigh denser than a bone however
    Low friction
      Less wear
      More range of motion
      Use Natural lubrication
    Ductile
      Like elongation, only matters if you jumped off of a building

## Slide 8
Isothermal Forging
  Cut ingot
  Heat ingot to 900ºC
  Fed into a hydraulic press
Heat treat
  Annealed
  700ºC for 1 hour
  Air cooled
Manufacturing: Forging
Notes:   Isothermal Forging
    Closed dye forging with equal temperature throughout process
    Cut an ingot to a precise length
    Heated to about 900ºC
    Die inserts (usually nickel) are heated to the forging temperature
    Fed into hydraulic press with a specific tool to form
      Have net shape
      Accurate precision
  Heat Treat of Isothermal Forging
    Annealed
    Temperature: 700ºC for 1 hour
    Air cooled, which allows for less deformation

## Slide 9
Hot-pressing in molds
  Loose powder placed into mold
  Heat and pressure are applied
  Occurs in a vacuum
Chemical/Heat Treat
  Product is grit blasted
  Passivation in nitric acid
  Placed in an alkaline solution
  Heat treated
    In air or vacuum
    At 600ºC
Manufacturing: Hot Press
Notes:   Hot-pressing in molds
    Loose powder placed into mold
      Powder uses 90% of raw material
      Can avoid/limit machining
      Used for materials with high melting point
      Hotter pressing temperature causes higher relative density
      Hotter pressing temperature causes higher hardness
    Occurs in a vacuum
  Chemical/Heat Treat after Hot-pressing
    Improves biocompatibility
      Reduces metal ion release
      Reduces water contact angle (increases wettability)
      Helps to absorb body fluids (containing proteins)
      Makes surface abrasive
      For plasma coating
    Passivation in nitric acid to remove any pathogens/diseases
    Placed in an alkaline solution to form oxide coating (termed anodize)
    Heat treated
      In air or vacuum
      At 600ºC

## Slide 10
Laser forming
Over 200 tons of semi-finished bars created
Other applications
  Orthopedics
  Dentistry
  Slinkys
  Airplane engines (I.E. fan blades)
Other Information
Notes: Recent experiment performed in 2012. Using a fine powder of Titanium Aluminum and Niobium. This is then inserted into a mold of the hip prosthesis and laser formed, over and over again till completed. This allows for a higher micron structure which in turn leads to less possibility of fractures or problems. This alloy is also used for knee, wrist and shoulder implants. Over 200 tons of semi-finished bars have been
http://www.jimrigby.org/wp-content/uploads/2012/03/slinky.jpg
created for mainly medical purposes of replacing parts in our bodies.

## Slide 11
Notes: Conclusion:
These are some of the applications of our alloy Ti-6Al-7Nb but the major one is the one in the middle for our particular research. If you think of all the ways we use our legs and hips each day it is perplexing how much wear and tear your body can take. One hundred years ago if your hip failed on you, you were a cripple possibly in a wheel chair. Now we have the ability to recreate your hip and you still have full control over it. We all take for granted our legs and how we can move whenever we want. This is why hip replacement is so amazing: it keeps people mobile so they can keep doing what they love.